## Slide 1: What science is there in welding?
Lars-Erik Svensson, University West, Engineering Science, Production West, Welding Technology

## Slide 2
Young PhD student
US Home security
What will you do in the US?
What kind of conference?
What subject?
What science is there in welding?
I will attend a conference
A scientific conference
Welding
Lars-Erik Svensson, University West, Engineering Science, Production West, Welding Technology

## Slide 3: What science is there in welding?
Mechanisation–control–quality-ergonomics–health&safety
Technology/science
High strength – low weight?
Process–material–design-heat–stresses–deformation–microstructure–properties
Economy
Lars-Erik Svensson, University West, Engineering Science, Production West, Welding Technology
High strength – low weight – long life?

## Slide 4: Technology/science
Lars-Erik Svensson, University West, Engineering Science, Production West, Welding Technology

## Slide 5: Technology/science
Lars-Erik Svensson, University West, Engineering Science, Production West, Welding Technology

## Slide 6: Technology/science
Lars-Erik Svensson, University West, Engineering Science, Production West, Welding Technology

## Slide 7: Technology/science
Lars-Erik Svensson, University West, Engineering Science, Production West, Welding Technology

## Slide 8: Technology/science
Lars-Erik Svensson, University West, Engineering Science, Production West, Welding Technology

## Slide 9: Technology/science
Lars-Erik Svensson, University West, Engineering Science, Production West, Welding Technology

## Slide 10: High strength – low weight
Steel (Fe – 0.2%C – 1% Mn – (0.5% Cr – 1% Ni – 0.5% Mo - 0.01 Ti/Nb/V)
Yield Strength 200 – 1100 MPa
(Stainless steel)
(Aluminium)
Lars-Erik Svensson, University West, Engineering Science, Production West, Welding Technology

## Slide 11: High strength – low weight
High strength of weld metal????
Lars-Erik Svensson, University West, Engineering Science, Production West, Welding Technology

## Slide 12: High strength – low weight
Lars-Erik Svensson, University West, Engineering Science, Production West, Welding Technology

## Slide 13: High strength – low weight
Lars-Erik Svensson, University West, Engineering Science, Production West, Welding Technology

## Slide 14: High strength – low weight
Microstructure - low and medium strength
GBF
AF
WF
Lars-Erik Svensson, University West, Engineering Science, Production West, Welding Technology

## Slide 15: High strength – low weight
Microstructure low – high strength
”Ferrite”
Bainite + Martensite
Yield Strength (MPa)
500 MPa 700 MPa 900 MPa
Lars-Erik Svensson, University West, Engineering Science, Production West, Welding Technology

## Slide 16: High strength – low weight
Chart: Yield strength (MPa)
| 425 | 450 | 500 | 550 | 600 | 650 | 700 | 750 | 800 | 850 | 900 | 950 | 1000
Mn-Ni | 70 | 80 | 105 | 130 | 123 | 115 | 110
Mn-Mo | 70 | 65 | 60 | 55 | 53 | 52 | 51
Toughness vs strength
Lars-Erik Svensson, University West, Engineering Science, Production West, Welding Technology

## Slide 17: High strength – low weight
Keehan
OK 75.78
0.5 Mn – 7 Ni
2 Mn – 7 Ni
Lars-Erik Svensson, University West, Engineering Science, Production West, Welding Technology

## Slide 18: High strength – low weight
Chart: Yield strength (MPa)
| 425 | 450 | 500 | 550 | 600 | 650 | 700 | 750 | 800 | 850 | 900 | 950 | 1000
Mn-Ni | 70 | 80 | 105 | 130 | 123 | 115 | 110
Mn-Mo | 70 | 65 | 60 | 55 | 53 | 52 | 51
low Mn-high Ni | 108 | 100 | 90 | 82 | 75
Lars-Erik Svensson, University West, Engineering Science, Production West, Welding Technology

## Slide 19: High strength – low weight - long life fatigue
Lars-Erik Svensson, University West, Engineering Science, Production West, Welding Technology

## Slide 20
Chart: Base metal tensile strength (MPa)
| 200 | 300 | 400 | 500 | 600 | 700
Non welded | 100 | 150 | 200 | 250 | 300 | 350
Welded | 100 | 100 | 100 | 100 | 100 | 100
High strength – low weight - long life fatigue
Lars-Erik Svensson, University West, Engineering Science, Production West, Welding Technology

## Slide 21: High strength – low weight - long life fatigue
Stress concentration
Defects
Residual stresses
Lars-Erik Svensson, University West, Engineering Science, Production West, Welding Technology

## Slide 22: High strength – low weight - long life fatigue
Conventional approaches: Improvement methods
Grinding (affects stress concentration, maybe defect occurrence)
TIG remelting (affects stress concentration, defect occurrence although not completely and residual stress)
Blasting/shot-peening/hammer peening (introduce compressive stress)
Lars-Erik Svensson, University West, Engineering Science, Production West, Welding Technology

## Slide 23: High strength – low weight - long life fatigue
Assuming a smooth weld without defects
Would we see:
Chart: Base metal tensile strength (MPa)
| 200 | 300 | 400 | 500 | 600 | 700
Non welded | 100 | 150 | 200 | 250 | 300 | 350
Welded | 100 | 105 | 110 | 115 | 120 | 125
?
Lars-Erik Svensson, University West, Engineering Science, Production West, Welding Technology

## Slide 24
What science is there in welding?
A lot Sir
But it’s impossible to explain for someone who don’t understand!*
Lars-Erik Svensson, University West, Engineering Science, Production West, Welding Technology
*Free translation of reply by Ingemar Stenmark, Swedens most famous downhill ski master, in a TV interview, on the question: Why did you not win today?