## Slide 1
Complete theory for martensitic transformations
www.msm.cam.ac.uk/phase-trans
Adolf Martens
memorial lecture

## Slide 2
Bain, Toriano, Wechsler, Liebermann,
Reed, Bowles, MacKenzie, Nishiyama,
Tamura, Shimizu, Kurdjumov,
Roitburd, Khandros, Cohen, Patel,
Krauss, Olson, Wayman, Zackay,
Wasserman, Christian, Bilby,
Hornbogen, Speich, Magee,
Koistinen, Marburger, Loretto, Ko

## Slide 7
The Bain strain

## Slide 8
[100]
[001]
o
a
a'
b
b'
o
b'
b
a,a'
(a)
(b)

## Slide 9
Austenite
(a)
w
x
y
z
Twinned
Martensite
Twin
Boundary
Correct macroscopic shape, correct structure
x
w
z
y
z
Slipped
Martensite
LATTICE
-INVARIANT
DEFORMATION
x
w
y
Observed
shape,
wrong
structure
P
(b)
w
x
z
y
1
RB
(c)
x
w
z
y
P
2
Martensite
(wrong
shape)

## Slide 11
transformation twins (Wayman)

## Slide 12
Martensite start temperature
Notes: 12

## Slide 13
athermal transformation

## Slide 14
Brooks, Loretto and Smallman, 1979

## Slide 15
However, martensitic transformation can be suppressed by rapid cooling to 4 K
Ullako et al.
1990

## Slide 18
Fe-0.1C wt%
Influence of tensile stress

## Slide 19
Bhadeshia, 1982

## Slide 20
s
50 mm
polycrystalline austenite
Bhadeshia, 1982

## Slide 21
Texture prediction

## Slide 22
No method calculates INTENSITY, only POSITIONS of poles

## Slide 23
TRIP steels that are fully austenitic are expensive
How do we produce cheap austenite?

## Slide 24: TRIP-Assisted Steels
too much carbon is bad
Jae Hoon Jang, In Gee Kim
austenite is expensive
carbon can be cheap
Notes: 24

## Slide 25
Typical composition Fe-0.15C-1.5Si-1.5Mn wt%

## Slide 28
tensile stress in fibre enclosed by matrix
Cracking of brittle martensite

## Slide 29
Chatterjee & Bhadeshia, 2006

## Slide 30
plates become finer than stress-transfer length, and hence do not crack

## Slide 31
plates stopped by austenite grain boundary
total volume transformed reduced when grain size small
detection limit leads to reduction in start temperature
Austenite grain size effects

## Slide 32
Yang & Bhadeshia, 2009

## Slide 33: Plastic strain: grain shape

## Slide 34: Plastic strain: stabilisation
Shipway & Bhadeshia 1995

## Slide 35: Plastic strain: stabilisation
Chatterjee & Bhadeshia

## Slide 36: Classic TRIP-assisted steel stress or strain-induced?

## Slide 37: Classic TRIP-assisted steel calculations of austenite stability

## Slide 38
Crystallography
Thermodynamics
Kinetics
Stress
Magnetic
Plastic strain
Interfacial structure
Texture
Critical mechanical properties
Chemical composition
Atomic structure

## Slide 40
Standard thermodynamic databases fail for epsilon martensite

## Slide 41
analysis limited to cases where

## Slide 42
Pure iron
CALPHAD
First principles
Fe-5Mn-2-Si-2Cr
First principles

## Slide 44
…………
empirical
method

## Slide 45
non-linear: neural networks